| PRODUCT TECHNICAL DATA SHEET |  |  | EA7-DMR-TDS- AKR07VDDBE |  |  |
| --- | --- | --- | --- | --- | --- |
| PRODUCT GROUP |  |  | AKR07 PMMA DISCS FOR REMOVABLE DENTURES |  |  |
| PRODUCT NAME |  |  | Villacryl DISC DB - PMMA disc for milling removable dentures bases Villacryl DISC Clear - PMMA disc for orthodontic appliance |  |  |
| PROJECT NUMBER (if applicable) |  |  | N/A |  |  |
| TF INDEX |  |  | EA7-TF-AKR07 |  |  |
| TECHNICAL SPECIFICATION |  |  | EA7-DMR ZN-25/25 "Villacryl DISC - acrylic discs for milling in CAD CAM technology" |  |  |
| Revision | Date | Change Reference |  | Prepared By | Description of Change |
| 1 | 2026-02-18 | N/A |  | Grzegorz Panas | First issue of document. |

| Physical form | Acrylic disc |
| --- | --- |
| Producer | Everall7 Sp. z o.o |
| Porosity | None |
| Flexural strength | >65 MPa |
| Flexural modulus | >2000 MPa |
| Sorption | < 32 µg/mm3 |
| Solubility | < 1,6 µg/mm3 |
| Residual methyl methacrylate monomer | max. 2,2% |
| Colour | A disc in shades of pink or transparent |
| Diameter | 98 ±0.5 mm |
| Total disk thickness | 20±0.25 mm 30 ±0.25 mm |
| Thickness of the rim to maintain | 10±0.25 mm |
| Package contain | 1 disc |

Approval of the product's Technical Data Sheet

|  | Signature | Date |
| --- | --- | --- |
| Grzegorz Panas R&D Manager |  | 2026-02-18 |
| Zbigniew Raszewski QA/RC Manager |  | 2026-02-18 |